## Slide 2: Chemical
Techniques and Developments
Mechanical
Planarization

## Slide 3: Chemical Mechanical Planarization Contents
What is CMP
The Mechanics of CMP
The Pad
The Slurry
What Can go Wrong
Future Developments
Notes: During mechanics, also note the modeling of CMP Processes

## Slide 4: What is Chemical Mechanical Planarization?
CMP creates very flat wafer surfaces for each new metal layer to be built upon
Historically a dirty process
Necessary for more than 3 metal layers
Devices Without Planrization
Planarized Circuit
Notes: Issues will arise when there is no planarization such as wells not getting filled properly and eventually non-connected deposited layers. Allows for accutate resist patterning, needed for smaller technologies.

## Slide 5: The Mechanics of Planarization
Forced against an abrasive pad with slurry
Gimbal point applies pressure onto wafer
Wafer placed upside down in carrier
Notes: Carrier Rotates around the gimabl point. The carrier film and the bottom pad are compresble to mainitain a uniform pressure.

## Slide 6: CMP Modeling – Preston’s Law
Top Pad
SiO2 Film to be Planarized
Abrasive Particles
Pressure on Wafer
Velocity of Wafer Relative to pad
Prestons’s Law: RR = (Kp)*(P)*(v)
RR: Removal Rate
P: Pressure
V: Velocity
Kp: Process Constant

## Slide 7: CMP Modeling – Preston’s Law
Prestons’s Law: RR = (Kp)*(P)*(v)
  Intuitive equation, generally valid for SiO2 polishing
Faster removal rate on less feature dense surface
Factors that go into the Kp term
  Film type/properties
  Abrasive particle details (size, amount, composition)
  Slurry variables (pH, composition, amount, viscosity)
  Temperature and pad variables
Notes: Often the Kp term is rather costant for a cetian process. Normal Pressure terms tend to be lass than 10 psi. V is typically between 50 and 500 meters per minute

## Slide 8: Rotary Polishing Devices
V = 2πrf
  Instantaneous Velocity
Not uniform abrasion across wafer
Better rotary polishing spins wafer and move across platen
Platen
Wafer Carrier
Slurry
Pad Cleaner
f

## Slide 9: Other Mechanical Polishing Techniques
Variations on rotary polishing
  Carousel and Orbital
Linier Polishing
  Constant Velocity
When is polishing complete?
  Time it
  Monitor motor current and vibrations
  Optical measurements
Wafer
Polishing Pad
v
Notes: Describe basic polishing techniques. Linier Constant velocity important for consistent polish.

## Slide 10: The Pad -- Characteristics
Must be hydrophilic (soaks liquid)
  Allows for pad/slurry reactions
Commonly made of Polyurethane
  Measured and predictable substance, chemically stable
Many pad varieties

## Slide 11: The Pad – Commonly Used Structures
Polyurethane foam with crater-like pores
Pad cured at high temperatures
Best for SiO2 polishing and better slurry loading
Micropourus Polymer Sheet
Grooved Pad Structure
Stiffer
Less slurry loading
Better for planarizing metals
All top pads rest on more flexible bottom pad

## Slide 12: The Pad – Variables affecting Removal Rate
Groove Designs – Spirals, Circles, Squares, Rays
  Prevents hydroplaning of wafer
  Allows slurry to penetrate whole wafer
Base Pad – Impacts curvature of top pad
Pad Thickness
  Determines stiffness of pad
  2x thickness = 8x stiffness
  Normally 1.3mm to 2.0mm thick
Notes: No grooves means nowhere for the slurry to go, also prevents edje effects. Planiarity quotient is the oxide removal rate at the bottom of a trench divided by the rate at the top.

## Slide 13: The Slurry – Purpose
Why do we need a slurry?
  Transporting waste particles from the wafer surface
  Abrasive particles
  Controlling pH and temperature
  Lubricating the pad and wafer
  Can etch one material faster then another with a specific slurry type
Two main slurry components are solution and solids
Notes: Other chemical effects are also presnt with the slurry

## Slide 14: Slurry Composition
Big mixture of chemicals
Surfactants
Inhibitors
Oxidizers
Other compounds
Particles that allow for a polishing effect on the wafer surface
Factors in removal rate include:
  Particle size (7-30 nm)
  Concentration (9-15%)
  Type (silica or alumina)
Solution
Solids
Solids in a slurry

## Slide 15: What goes wrong -- Dishing
Dishing is a dip in metal lines caused by over-polishing and slurry composition
  Results in decreased average thickness
  Increased line resistivity
  Reduced signal propagation speeds
  Decreases overall planarity
Can be prevented with precise CMP timing or optical sensing
  -- If many metal vias are in a row, erosion can occure
Notes: Some modern slurry compositions have a 1:1 etch rate for oxide and metal, which can prevent some issues, but not all. The analysis gets more complex since most vias are coated with a film of titmnium, which will be etched at a differnet rate then either copper or oxide.

## Slide 16: Future CMP Advancements

## Slide 17: Works Cited

## Slide 18: Hidden Feature